ECO/TN   Marina Holbrook	ECO/IC

Dr. Linda Park

Tel.  +1 302 555-0162

Date  14-03-2022

Report-no:  US2022-0184

640000167432

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Polyester Powder Coat Reference Standard #R3217; 020003691402

Polyester Powder Coat #30024781503; 020003691404

Polyester Powder Coat #30024781504; 020003691406

Polyester Powder Coat #30024781505; 020003691408

Receipt of order:  06-03-2022

1.  General introduction

On 14-03-2022, our laboratory received four samples submitted by Cascade Mountain Coatings Co. for compositional analysis of polyester powder coat material. The samples comprise one reference standard and three production batches, provided for verification against internal release specifications. The following investigations were performed:

- Determination of ash content by gravimetric analysis at elevated temperature.

- Identification and quantification of metallic constituents by ICP-OES.

- Qualitative elemental confirmation by X-ray fluorescence (XRF).

- Determination of softening point by ring-and-ball method.

- Characterisation of binder system by FTIR.

2.  Sample preparation

2.1  Sample preparation for elemental analysis

Approximately 0.25 g of each powdered sample was digested in a closed-vessel microwave digestion system using a mixture of 6 mL concentrated nitric acid (HNO₃, 65%) and 2 mL hydrochloric acid (HCl, 37%). The digestion programme reached a maximum temperature of 200 °C and was held for 20 minutes. After cooling, the digests were diluted to 50 mL with ultrapure water prior to ICP-OES analysis.

2.2  Sample preparation for XRF and softening point

Powdered sub-samples were pressed into 32 mm pellets using a hydraulic press at 15 tons. Softening points were determined by the standard ring-and-ball method using a heating rate of 5 °C/min.

3.  Results

3.1  Composition (elemental, transposed format)

Results are presented with samples as rows and parameters as columns for ease of cross-sample reading. All elemental values are mass percentages (% w/w).

| Sample | Ash [%] | Ti [%] | Al [%] | Si [%] | Ca [%] | Fe [%] | Zn [%] | XRF qual. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Reference Standard #R3217; 020003691402 | 0.5 | 0.04 | 0.02 | 0.07 | < 0.01 | < 0.01 | 0.01 | Ti, Si |
| #30024781503; 020003691404 | 9.8 | 2.14 | 0.31 | 0.78 | 1.84 | 0.04 | 0.42 | Ti, Al, Si, Ca, Fe, Zn |
| #30024781504; 020003691406 | 9.6 | 2.18 | 0.29 | 0.74 | 1.79 | 0.03 | 0.44 | Ti, Al, Si, Ca, Fe, Zn |
| #30024781505; 020003691408 | 9.9 | 2.11 | 0.32 | 0.81 | 1.88 | 0.04 | 0.40 | Ti, Al, Si, Ca, Fe, Zn |

3.2  Binder characterisation

The four submitted samples were characterised by FTIR in the spectral range 4000–650 cm⁻¹. All samples exhibited absorption profiles consistent with a polyester binder system, with characteristic ester carbonyl C=O stretches at 1718 cm⁻¹ and aromatic C=C stretches at 1605 cm⁻¹. No significant batch-to-batch deviation was observed. Softening points (104–106 °C) are within the historical baseline for this product line. All elemental parameters are within internal specification, and the product as supplied meets release criteria.

Costs of analysis:  1,420.00 USD