ECO/TN   Anthony Russo	ECO/AC

Dr. Samuel Whitaker

Tel.  +1 302 555-0148

Date  26-08-2022

Report-no:  US2022-0721

640000179218

Confidential – only for internal use!

Result of the analytical investigation of the samples:

2K-PU Clearcoat Reference Standard; 020003738201

2K-PU Clearcoat (internal code PU-A); 020003738203

2K-PU Clearcoat (internal code PU-B); 020003738205

2K-PU Clearcoat (internal code PU-C); 020003738207

Date of request:  12-08-2022

Receipt of order:  18-08-2022

1.  General introduction

On 26-08-2022, our laboratory received four samples submitted by Crestline Auto Refinish for analytical characterisation. The samples were submitted under internal coding (PU-A, PU-B, PU-C) at the customer's request, with full batch numbers retained at customer's premises. The following investigations were performed:

- Determination of ash content by gravimetric analysis.

- Identification of inorganic constituents by ICP-OES on total material.

- Qualitative elemental confirmation by XRF.

- Determination of water-soluble components by ICP-OES on aqueous extract.

- Characterisation of binder by FTIR; silicone oil determination by ¹H-NMR.

2.  Sample preparation

2.1  Sample preparation for ICP-OES on total material

Approximately 0.25 g of each sample was digested in a closed-vessel microwave digestion system using a mixture of HNO₃ and HCl at 200 °C for 20 minutes. After cooling, digests were diluted to 50 mL with ultrapure water for analysis.

2.2  Sample preparation for ICP-OES on aqueous extract

Approximately 5 g of each sample was extracted with 100 mL of ultrapure water at 80 °C for two hours under continuous stirring. Extracts were filtered through 0.22 µm membranes and acidified with 1% HNO₃ prior to analysis.

2.3  Sample preparation for FTIR and ¹H-NMR

Solvent extracts were prepared using a 4:1 (v/v) dichloromethane/methanol mixture under reflux. Aliquots of 100 mg were extracted with 1.0 mL of CDCl₃ for NMR characterisation at 400 MHz.

3.  Results

3.1  Inorganic composition (parameter-value listing)

Each parameter is presented with its reference standard value and the corresponding values from the three internal-coded batches.

| Parameter | Values (Reference + 3 internal codes) |
| --- | --- |
| Ash content (600 °C) [%] | Reference: 0.8 PU-A: 12.4 PU-B: 12.6 PU-C: 12.3 |
| Titanium [%] | Reference: 0.05 PU-A: 2.79 PU-B: 2.86 PU-C: 2.74 |
| Aluminium [%] | Reference: 0.02 PU-A: 0.44 PU-B: 0.47 PU-C: 0.42 |
| Silicon [%] | Reference: 0.08 PU-A: 1.19 PU-B: 1.14 PU-C: 1.24 |
| Calcium [%] | Reference: < 0.01 PU-A: 3.10 PU-B: 3.02 PU-C: 3.17 |
| Magnesium [%] | Reference: < 0.01 PU-A: 0.18 PU-B: 0.21 PU-C: 0.16 |
| Iron [%] | Reference: < 0.01 PU-A: 0.06 PU-B: 0.07 PU-C: 0.06 |
| Zinc [%] | Reference: 0.01 PU-A: 0.71 PU-B: 0.68 PU-C: 0.74 |
| Barium [%] | Reference: n.d. PU-A: 4.28 PU-B: 4.07 PU-C: 4.44 |
| Sulphur [%] | Reference: < 0.01 PU-A: 1.11 PU-B: 0.99 PU-C: 1.18 |

3.2  Aqueous extract analysis

| Parameter (aqueous extract) | Values [mg/L] |
| --- | --- |
| Sodium | Reference: 2.1 PU-A: 8.6 PU-B: 8.4 PU-C: 8.8 |
| Potassium | Reference: 0.8 PU-A: 3.3 PU-B: 3.1 PU-C: 3.5 |
| Calcium | Reference: 1.2 PU-A: 6.4 PU-B: 6.7 PU-C: 6.2 |
| Magnesium | Reference: 0.3 PU-A: 1.7 PU-B: 1.6 PU-C: 1.8 |
| Chloride | Reference: 1.5 PU-A: 4.1 PU-B: 3.9 PU-C: 4.3 |
| Sulphate | Reference: 0.9 PU-A: 5.7 PU-B: 5.5 PU-C: 5.9 |

3.3  Binder characterisation and findings

The solvent extracts of the four samples were characterised by FTIR. All samples displayed absorption profiles consistent with a 2K-PU binder system. Iron content (0.06–0.07%) is at the historical baseline for this product line and well within the 0.10% internal specification. ¹H-NMR analysis confirmed the absence of silicone oil contamination above the method detection limit. The product as supplied meets release criteria.

Costs of analysis:  1,490.00 USD