ECO/TN   Patricia Hayes	ECO/PC

Dr. James Holloway

Tel.  +1 302 555-0174

Date  11-04-2023

Report-no:  US2023-0394

640000201548

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Alkyd Enamel Reference Standard #R4108; 020003781901

Alkyd Enamel #30041287618

Alkyd Enamel #30041287619

Alkyd Enamel #30041287620

Date of request:  28-03-2023

Receipt of order:  04-04-2023

1.  General introduction

On 11-04-2023, our laboratory received four samples submitted by Tidewater Industrial Finishes Ltd. for batch release analysis of alkyd enamel material. The samples comprise one reference standard and three production batches. Sample identifiers for the production batches were not provided at intake; reporting is by batch number only. The following investigations were performed:

- Determination of solids content by gravimetric analysis.

- Identification of inorganic constituents by ICP-OES.

- Determination of water-soluble ionic components by ion chromatography.

- Characterisation of binder system by FTIR.

- Determination of drying time per ASTM D5895.

2.  Sample preparation

2.1  Solids content determination

Approximately 1 g of each sample was weighed into pre-tared aluminium dishes and dried in a forced-air oven at 110 °C for 60 minutes. After cooling in a desiccator, dry mass was recorded and solids content calculated as % w/w.

2.2  Sample preparation for ICP-OES

Approximately 0.25 g of each sample was digested using HNO₃/HCl (3:1) in a closed-vessel microwave at 200 °C for 20 minutes; digests were diluted to 50 mL with ultrapure water.

2.3  Sample preparation for ion chromatography

Approximately 5 g of each sample was extracted with 50 mL of deionised water at room temperature for 24 hours, filtered through a 0.45 µm PES membrane, and analysed directly by ion chromatography.

3.  Results

3.1  Solids content and elemental composition

Solids content and metallic constituents are presented in the table below. All values for elements are mass percentages (% w/w).

|  | Reference Standard #R4108 | #30041287618 | #30041287619 | #30041287620 |
| --- | --- | --- | --- | --- |
| Solids content [%] | 62.4 | 58.1 | 57.8 | 58.4 |
| Iron (Fe) [%] | 0.04 | 0.05 | 0.04 | 0.05 |
| Aluminium [%] | 0.02 | 0.03 | 0.02 | 0.03 |
| Silicon (Si) [%] | 0.06 | 0.08 | 0.07 | 0.08 |
| Calcium [%] | 0.41 | 0.38 | 0.40 | 0.39 |
| Zinc (Zn) [%] | 0.18 | 0.21 | 0.19 | 0.22 |
| Lead [%] | < 0.001 | < 0.001 | < 0.001 | < 0.001 |

3.2  Aqueous extract — ionic content

Chloride, sulphate, nitrate, and pH are reported separately for the aqueous extract.

|  | Reference Standard #R4108 | #30041287618 | #30041287619 | #30041287620 |
| --- | --- | --- | --- | --- |
| Chloride [mg/L] | 0.04 | 0.05 | 0.04 | 0.05 |
| Sulphate [mg/L] | 0.18 | 0.21 | 0.19 | 0.20 |
| Nitrate [mg/L] | < 0.10 | 0.12 | 0.11 | 0.13 |
| pH (1:10 extract) | 7.8 | 8.0 | 7.9 | 8.0 |

3.3  Binder system and drying performance

The four samples were characterised by FTIR in the spectral range 4000–650 cm⁻¹. The reference and three batches displayed absorption profiles consistent with an alkyd resin binder system. NOTE: Solids content in production batches (57.8–58.4%) falls below the internal specification of 60.0% minimum, with the reference at 62.4%. The reduction translates to approximately 6–7% under-bodied product, which will affect customer film build and drying time. ASTM D5895 dry-to-touch times for the production batches (5.5–6.0 hours) exceed the typical specification of 4.0 hours. Recommended action: review the resin let-down ratio and the solvent dosing on the production line; release of these batches should be held pending review.

Costs of analysis:  1,560.00 USD