ECO/TN   Robert Schwartz	ECO/SP

Dr. Rachel Mendez

Tel.  +1 302 555-0156

Date  19-07-2023

Report-no:  US2023-0512

640000208719

Confidential – only for internal use!

Result of the analytical investigation of the samples:

WB Basecoat Reference Standard #R4319; 020003802101

WB Basecoat #30043912508; 020003802103

Date of request:  06-07-2023

Receipt of order:  12-07-2023

1.  General introduction

On 19-07-2023, our laboratory received two samples for in-depth analytical characterisation of a single production batch against the reference standard. The submission originates from a customer site in Detroit, MI; account code reference was not provided. This deep-dive analysis includes the standard parameter set extended with rheological and visual-quality measurements. The following investigations were performed:

- Determination of ash content by gravimetric analysis.

- Quantification of metallic constituents by ICP-OES (Fe, TiO₂, Al, SiO₂, Ca, Mg, Zn).

- Determination of 60° gloss per ASTM D523.

- Brookfield viscosity measurement at 25 °C.

- pH of the aqueous extract.

- Characterisation of binder system by FTIR.

2.  Sample preparation

2.1  Sample preparation for elemental analysis

Approximately 0.25 g of each sample was digested in a closed-vessel microwave system using a mixture of HNO₃ (6 mL) and HCl (2 mL) at 200 °C for 20 minutes. After cooling, the digests were diluted to 50 mL with ultrapure water for analysis.

2.2  Sample preparation for gloss, viscosity, and pH

Drawdowns for gloss measurement were prepared at 100 µm wet film thickness on Leneta sealed black/white cards and dried for 24 hours under controlled humidity conditions. Brookfield viscosity was measured directly on the as-supplied liquid sample using spindle LV-3 at 60 rpm. pH was measured on an aqueous extract prepared at 1:10 dilution.

3.  Results

3.1  Single-batch analytical comparison

All analytical parameters for the reference and production batch are presented below. Mass percentages are reported as % w/w; gloss is in gloss units (GU); viscosity in mPa·s.

| Parameter | Reference #R4319; 020003802101 | Production #30043912508; 020003802103 |
| --- | --- | --- |
| Ash content (600 °C) [%] | 0.6 | 8.7 |
| Fe [%] | < 0.01 | 0.05 |
| TiO₂ [%] | 0.04 | 4.21 |
| Al [%] | 0.01 | 0.31 |
| SiO₂ [%] | 0.04 | 0.86 |
| Ca [%] | < 0.01 | 1.42 |
| Mg [%] | < 0.01 | 0.10 |
| Zn [%] | 0.01 | 0.36 |
| 60° Gloss [GU] | 92 | 89 |
| Brookfield viscosity [mPa·s, 25 °C] | 180 | 184 |
| pH (aqueous extract) | 8.2 | 8.3 |

3.2  Binder system and overall assessment

The solvent extract of the production batch and reference standard were characterised by FTIR in the spectral range 4000–650 cm⁻¹. Both samples displayed absorption profiles consistent with a waterborne acrylic-urethane basecoat system. The 60° gloss reading for the production batch (89 GU) is within the acceptable tolerance vs the reference (92 GU). Brookfield viscosity (184 mPa·s) and pH (8.3) are both within historical baseline. All metallic constituents fall within internal specification. The single submitted batch meets release criteria for shipment.

Costs of analysis:  1,640.00 USD