ECO/TN   Karen O'Sullivan	ECO/IC

Dr. Linda Park

Tel.  +1 302 555-0162

Date  20-10-2023

Report-no:  US2023-0824

640000222431

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Epoxy Topcoat Reference Standard #R4527; 020003824701

Epoxy Topcoat #30048312715; 020003824703

Epoxy Topcoat #30048312716; 020003824705

Epoxy Topcoat #30048312717; 020003824707

Receipt of order:  12-10-2023

1.  General introduction

On 20-10-2023, our laboratory received four samples submitted by Cascade Mountain Coatings Co. for batch release analysis of epoxy topcoat material. The samples comprise one reference standard and three production batches, presented for verification against internal release specifications. Status against specification is shown alongside each measured value. The following investigations were performed:

- Quantification of inorganic oxide constituents by ICP-OES (results expressed as oxides).

- Determination of ash residue at 600 °C.

- Qualitative XRF screening for trace contamination.

- Determination of pendulum hardness per ASTM D4366.

- Characterisation of epoxy binder by FTIR.

2.  Sample preparation

2.1  Sample preparation for ICP-OES (oxide reporting)

Approximately 0.20 g of each sample was digested in a closed-vessel microwave system using a mixture of concentrated HNO₃ (6 mL) and HF (1 mL) at 220 °C for 30 minutes. Element concentrations measured by ICP-OES were converted stoichiometrically to oxide equivalents and reported as % w/w.

2.2  Sample preparation for ash and pendulum hardness

Ash content was determined gravimetrically after thermal treatment at 600 °C. Pendulum hardness drawdowns were prepared at 50 µm dry film thickness on glass plates and conditioned for 7 days at 23 °C / 50% RH prior to measurement per ASTM D4366.

3.  Results

3.1  Composition with PASS/FAIL status (oxide reporting)

Each parameter is presented with its specification limit, the reference standard value, the values for the three production batches, and an explicit pass/fail status. Mass percentages are reported as % w/w.

| Parameter | Spec | Ref Std #R4527 | #30048312715 | #30048312716 | #30048312717 | Status |
| --- | --- | --- | --- | --- | --- | --- |
| TiO₂ [%] | max 25.0 | 0.05 | 21.84 | 21.91 | 21.78 | PASS |
| Fe₂O₃ [%] | max 0.30 | < 0.01 | 0.18 | 0.22 | 0.19 | PASS |
| Al₂O₃ [%] | max 1.00 | 0.04 | 0.62 | 0.59 | 0.64 | PASS |
| SiO₂ [%] | max 2.00 | 0.09 | 1.31 | 1.28 | 1.34 | PASS |
| CaO [%] | max 5.00 | < 0.01 | 3.02 | 3.11 | 2.94 | PASS |
| MgO [%] | max 0.50 | < 0.01 | 0.18 | 0.21 | 0.17 | PASS |
| BaO [%] | max 6.00 | n.d. | 4.18 | 4.07 | 4.32 | PASS |
| Ash content [%] | — | 0.7 | 11.8 | 12.1 | 11.6 | — |
| Pendulum hardness [s] | min 110 | — | 118 | 121 | 115 | PASS |

3.2  Binder system and release determination

The four samples were characterised by FTIR in the spectral range 4000–650 cm⁻¹. All samples displayed absorption profiles consistent with a bisphenol A epoxy resin binder system, with the characteristic aromatic stretches at 1606 and 1508 cm⁻¹ and the epoxide ring deformation at 915 cm⁻¹. All measured oxide constituents are within internal specification limits. Pendulum hardness (115–121 s) exceeds the 110 s minimum specification. All three production batches PASS internal release criteria. The product as supplied is suitable for shipment.

Costs of analysis:  1,720.00 USD