ECO/TN Jacob Haiser	ECO/PC

Dr. James Holloway

Tel.  +1 302 555-0174

Date  13-12-2023

Report-no:  US2023-0958

640000228547

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Zinc-Rich Epoxy Primer Reference Standard #R4682; 020003844201

Zinc-Rich Epoxy Primer #30053418204; 020003844203

Zinc-Rich Epoxy Primer #30053418205; 020003844205

Zinc-Rich Epoxy Primer #30053418206; 020003844207

Date of request:  29-11-2023

Receipt of order:  06-12-2023

1.  General introduction

On 13-12-2023, our laboratory received four samples submitted by Tidewater Industrial Finishes Ltd. for routine batch release analysis of zinc-rich epoxy primer intended for marine application. The samples comprise one reference standard and three production batches. Each sample is reported in its own dedicated section with parameter values, allowing direct one-batch-at-a-time review. Trace metallic constituents are reported in ppm. The following investigations were performed:

- Determination of zinc content and metallic composition by ICP-OES.

- Determination of ash content.

- Determination of chloride and sulphate by ion chromatography on aqueous extract.

- Qualitative elemental confirmation by XRF.

- Characterisation of epoxy binder by FTIR.

2.  Sample preparation

2.1  Acid digestion for ICP-OES

Approximately 0.25 g of each sample was digested in a closed-vessel microwave system using a mixture of HNO₃ (6 mL) and HCl (2 mL) at 200 °C for 20 minutes. Trace metals (Pb, Cd, Cr) were quantified at ppm-level using a separate matrix-matched calibration.

2.2  Aqueous extraction for ion chromatography

Approximately 5 g of each sample was extracted with 100 mL of ultrapure water at 80 °C for two hours under continuous stirring; extracts were filtered through a 0.22 µm membrane prior to ion chromatography for chloride and sulphate.

3.  Results

3.1  Per-sample analytical summary (vertical stacked)

Results are presented one sample at a time, with each sample's full parameter set in its own dedicated mini-table. Trace metals (Pb, Cd, Cr) reported in ppm; bulk constituents in mass percentage; ionic species in mg/L from aqueous extract.

| Sample 1 — Reference Standard #R4682; 020003844201 |
| --- |
| Zinc [%] | 82.4 |
| Iron [%] | 0.18 |
| Aluminium [%] | 0.42 |
| Silicon [%] | 0.61 |
| Calcium [%] | 0.08 |
| Magnesium [%] | 0.04 |
| Lead [ppm] | < 10 |
| Cadmium [ppm] | < 5 |
| Chromium [ppm] | < 8 |
| Chloride [mg/L] | 0.04 |
| Sulphate [mg/L] | 0.12 |
| Ash content (600 °C) [%] | 62.4 |
| pH (aqueous extract) | 8.4 |

| Sample 2 — #30053418204; 020003844203 |
| --- |
| Zinc [%] | 82.1 |
| Iron [%] | 0.21 |
| Aluminium [%] | 0.41 |
| Silicon [%] | 0.63 |
| Calcium [%] | 0.07 |
| Magnesium [%] | 0.04 |
| Lead [ppm] | < 10 |
| Cadmium [ppm] | < 5 |
| Chromium [ppm] | < 8 |
| Chloride [mg/L] | 0.12 |
| Sulphate [mg/L] | 0.14 |
| Ash content (600 °C) [%] | 62.1 |
| pH (aqueous extract) | 8.5 |

| Sample 3 — #30053418205; 020003844205 |
| --- |
| Zinc [%] | 82.6 |
| Iron [%] | 0.19 |
| Aluminium [%] | 0.43 |
| Silicon [%] | 0.60 |
| Calcium [%] | 0.08 |
| Magnesium [%] | 0.04 |
| Lead [ppm] | < 10 |
| Cadmium [ppm] | < 5 |
| Chromium [ppm] | < 8 |
| Chloride [mg/L] | 0.11 |
| Sulphate [mg/L] | 0.13 |
| Ash content (600 °C) [%] | 62.7 |
| pH (aqueous extract) | 8.4 |

| Sample 4 — #30053418206; 020003844207 |
| --- |
| Zinc [%] | 82.3 |
| Iron [%] | 0.22 |
| Aluminium [%] | 0.40 |
| Silicon [%] | 0.62 |
| Calcium [%] | 0.09 |
| Magnesium [%] | 0.05 |
| Lead [ppm] | < 10 |
| Cadmium [ppm] | < 5 |
| Chromium [ppm] | < 8 |
| Chloride [mg/L] | 0.13 |
| Sulphate [mg/L] | 0.13 |
| Ash content (600 °C) [%] | 62.3 |
| pH (aqueous extract) | 8.5 |

3.2  Findings and release determination

The four samples were characterised by ICP-OES, ion chromatography, and FTIR. Zinc content (82.1–82.6%) exceeds the minimum specification of 80% across all production batches. Iron, lead, and cadmium are well within RoHS limits. The binder system is consistent with bisphenol A epoxy resin in all samples. NOTE: Chloride content in the production batches (0.11/0.12/0.13 mg/L) is at or above the 0.10 mg/L specification limit for marine application. While the elevation is modest, these batches should be flagged for review before shipment to offshore environments. Recommended action: review production-water chloride content and the rinse-water specification at the dispersion line.

Costs of analysis:  1,790.00 USD