ECO/TN   Patricia Hayes	ECO/SP

Dr. Rachel Mendez

Tel.  +1 302 555-0156

Date  22-05-2024

Report-no:  US2024-0468

640000249108

Confidential – only for internal use!

Result of the analytical investigation of the samples:

2K-PU Clearcoat Reference Standard #R4756; 020003872104

2K-PU Clearcoat #30062418207; 020003872106

2K-PU Clearcoat #30062418208; 020003872108

2K-PU Clearcoat #30062418209; 020003872110

Date of request:  10-05-2024

Receipt of order:  14-05-2024

1.  General introduction

On 22-05-2024, our laboratory received four samples submitted by Apex Surface Solutions for comprehensive analytical characterisation. The samples comprise one reference standard and three production batches of 2K-PU clearcoat, provided for comparative compositional analysis against internal specifications and customer release criteria. In order to fully characterise the submitted materials, the following investigations were performed:

- Determination of ash content by gravimetric analysis at elevated temperature.

- Identification and quantification of inorganic constituents in the total material by inductively coupled plasma optical emission spectrometry (ICP-OES).

- Qualitative elemental screening of the total material by X-ray fluorescence spectroscopy (XRF).

- Determination of water-soluble inorganic components in the aqueous extract by ICP-OES.

- Characterisation of organic coating fractions by Fourier-transform infrared spectroscopy (FTIR).

- Determination of silicone oil content by proton nuclear magnetic resonance spectroscopy (¹H-NMR).

2.  Sample preparation

2.1  Sample preparation for gravimetric and spectroscopic analysis

2.1.1  Examination of total material

Approximately 2 g of each sample was weighed into pre-ignited porcelain crucibles using a calibrated analytical balance with a readability of 0.1 mg. The samples were subjected to controlled thermal treatment in a muffle furnace under atmospheric conditions, with target temperatures selected on the basis of the thermal stability characteristics of each material. The residual ash content was determined gravimetrically after cooling the crucibles in a desiccator to constant weight.

2.1.2  Analysis of organic coating

The organic coating fraction was separated from the total material by solvent extraction using a 4:1 (v/v) dichloromethane/methanol mixture under reflux for four hours. The extracts were filtered through 0.45 µm PTFE membranes, concentrated under reduced pressure, and transferred to sample holders for subsequent spectroscopic characterisation by FTIR.

2.2  Sample preparation for elemental analysis (ICP-OES)

2.2.1  Sample preparation for optical emission spectrometry on total material

Approximately 0.25 g of each sample was digested in a closed-vessel microwave digestion system using a mixture of 6 mL concentrated nitric acid (HNO₃, 65%) and 2 mL hydrochloric acid (HCl, 37%). The digestion programme reached a maximum temperature of 200 °C and was held for 20 minutes. After cooling, the clear digests were quantitatively transferred and diluted to 50 mL with ultrapure water (≥ 18.2 MΩ·cm) prior to analysis.

2.2.2  Sample preparation for optical emission spectrometry on aqueous extract

A portion of each sample (approximately 5 g) was extracted with 100 mL of ultrapure water at 80 °C for two hours under continuous magnetic stirring. The extracts were cooled to room temperature, filtered through 0.22 µm cellulose acetate membrane filters, and acidified with 1 % (v/v) nitric acid to preserve dissolved species prior to ICP-OES analysis.

2.3  Sample preparation for the X-ray fluorescence analysis on the total material

Finely ground sub-samples were prepared by cryogenic milling to ensure complete homogenisation and a consistent particle size distribution below 50 µm. Approximately 4 g of the milled material was then pressed into 32 mm pellets using a hydraulic press operating at 15 tons for 60 seconds, with cellulose binder mixed in a 4:1 sample-to-binder ratio. The pressed pellets were analysed directly in the XRF instrument under vacuum conditions (< 10 mbar) using a rhodium anode X-ray tube operated at 50 kV and 40 mA.

3.  Results

3.1  Inorganic analysis

The inorganic constituents of the four submitted samples were characterised by a combination of gravimetric and spectroscopic techniques. The results of the ash content determination and subsequent elemental analyses are summarised below.

|  | 2K-PU Clearcoat Reference Standard #R4756; 020003872104 | 2K-PU Clearcoat #30062418207; 020003872106 | 2K-PU Clearcoat #30062418208; 020003872108 | 2K-PU Clearcoat #30062418209; 020003872110 |
| --- | --- | --- | --- | --- |
| Ash content (600 °C) [%] | 0.8 | 12.6 | 12.3 | 12.7 |

3.1.1  Composition of the total material

The acid digests of the four samples were analysed for their elemental composition by ICP-OES. All quantitative values are expressed as mass percentage (% w/w) relative to the original sample mass.

The following elements were detected by ICP-OES:

|  | 2K-PU Clearcoat Reference Standard #R4756; 020003872104 | 2K-PU Clearcoat #30062418207; 020003872106 | 2K-PU Clearcoat #30062418208; 020003872108 | 2K-PU Clearcoat #30062418209; 020003872110 |
| --- | --- | --- | --- | --- |
| Titanium (Ti) | 0.05 % | 2.86 % | 2.98 % | 2.76 % |
| Aluminium (Al) | 0.02 % | 0.47 % | 0.50 % | 0.45 % |
| Silicon (Si) | 0.08 % | 1.24 % | 1.18 % | 1.30 % |
| Calcium (Ca) | < 0.01 | 3.16 % | 3.08 % | 3.23 % |
| Magnesium (Mg) | < 0.01 | 0.20 % | 0.23 % | 0.19 % |
| Iron (Fe) | < 0.01 | 0.16 % | 0.15 % | 0.17 % |
| Zinc (Zn) | 0.01 % | 0.74 % | 0.70 % | 0.77 % |
| Barium (Ba) | n.d. | 4.36 % | 4.15 % | 4.53 % |
| Sulphur (S) | < 0.01 | 1.18 % | 1.06 % | 1.25 % |
| Qualitatively detected elements by XRF | Ti, Si, Ca, Zn | Ti, Al, Si, Ca, Mg, Fe, Zn, Ba, S | Ti, Al, Si, Ca, Mg, Fe, Zn, Ba, S | Ti, Al, Si, Ca, Mg, Fe, Zn, Ba, S |

3.1.2  Analysis of inorganic water-soluble components

The following elements could be determined in the aqueous extract:

|  | 2K-PU Clearcoat Reference Standard #R4756; 020003872104 | 2K-PU Clearcoat #30062418207; 020003872106 | 2K-PU Clearcoat #30062418208; 020003872108 | 2K-PU Clearcoat #30062418209; 020003872110 |
| --- | --- | --- | --- | --- |
| Sodium (Na) | 2.1 mg/l | 8.7 mg/l | 8.5 mg/l | 8.9 mg/l |
| Potassium (K) | 0.8 mg/l | 3.4 mg/l | 3.2 mg/l | 3.6 mg/l |
| Calcium (Ca) | 1.2 mg/l | 6.5 mg/l | 6.8 mg/l | 6.3 mg/l |
| Magnesium (Mg) | 0.3 mg/l | 1.8 mg/l | 1.7 mg/l | 1.9 mg/l |
| Chloride (Cl⁻) | 1.5 mg/l | 4.2 mg/l | 4.0 mg/l | 4.4 mg/l |
| Sulphate (SO₄²⁻) | 0.9 mg/l | 5.8 mg/l | 5.6 mg/l | 6.0 mg/l |
| Nitrate (NO₃⁻) | < 0.1 mg/l | 0.7 mg/l | 0.6 mg/l | 0.8 mg/l |
| Qualitatively detected elements in the trace range (c < 0.1 mg/l) | Sr, Li, B | Sr, Li, B, Mn, Ba | Sr, Li, B, Mn, Ba | Sr, Li, B, Mn |

3.2  Organic coatings

The solvent extracts of the four submitted samples were characterised by Fourier-transform infrared spectroscopy in the spectral range 4000–650 cm⁻¹. The reference and three production batches displayed spectra consistent with a 2K-PU binder system, with no significant variation in the binder fingerprint region. Iron content in the production batches (0.16 / 0.15 / 0.17 %) exceeds the internal specification limit of 0.10 % and continues the upward trend observed since mid-2023. Recommend escalation to the quality assurance team for review of supplier raw material certificates and a check of the pigment dispersion equipment. Cross-batch consistency suggests a systemic input source rather than a sporadic contamination event.

3.3  Determination of silicone oil contents by Proton-NMR

For the quantitative determination of silicone oil, aliquots of approximately 100 mg of each sample were extracted with 1.0 mL of deuterated chloroform (CDCl₃) containing tetramethylsilane (TMS) as internal chemical shift reference. Analyses were performed on a 400 MHz ¹H-NMR spectrometer under standard acquisition conditions (128 scans, relaxation delay of 5 s). Polydimethylsiloxane (PDMS), the principal component of silicone oils typically encountered in coating matrices, produces a characteristic singlet at approximately 0.07 ppm arising from the Si–CH₃ protons. In the relevant chemical shift range (0.00–0.15 ppm), a weak singlet at 0.07 ppm was observed in the reference clearcoat, indicating the presence of silicone oil at trace levels below the quantification limit, consistent with the use of silicone-based levelling additives in clearcoat formulations. No corresponding signals were detected in any of the three 2K-PU clearcoat batches, confirming the absence of silicone oil contamination. The limit of detection (LOD) and limit of quantification (LOQ) of the method were established at 5 mg/kg and 15 mg/kg, respectively.

Costs of analysis:  1,545.00 USD