ECO/TN   Caroline Dunn	ECO/AC

Dr. Samuel Whitaker

Tel.  +1 302 555-0148

Date  04-09-2025

Report-no:  US2025-0547

640000308197

Confidential – only for internal use!

Result of the analytical investigation of the samples:

WB Acrylic Emulsion Reference Standard #R5798; 020003954801

WB Acrylic Emulsion #30084218501; 020003954803

WB Acrylic Emulsion #30084218502; 020003954805

WB Acrylic Emulsion #30084218503; 020003954807

Date of request:  21-08-2025

Receipt of order:  28-08-2025

1.  General introduction

On 04-09-2025, our laboratory received four samples submitted by Vanguard Industrial Paints for compositional analysis. The samples comprise one reference standard and three production batches of waterborne acrylic emulsion, provided for verification against internal specifications and customer release criteria. The following investigations were performed:

- Determination of ash content by gravimetric analysis at elevated temperature.

- Identification and quantification of inorganic constituents by ICP-OES.

- Qualitative elemental screening by X-ray fluorescence (XRF).

- Determination of water-soluble inorganic components by ICP-OES on aqueous extract.

- Characterisation of binder system by FTIR and silicone oil determination by ¹H-NMR.

2.  Sample preparation

2.1  Sample preparation for gravimetric and spectroscopic analysis

2.1.1  Examination of total material

Approximately 2 g of each sample was weighed into pre-ignited porcelain crucibles using a calibrated analytical balance with a readability of 0.1 mg. The samples were subjected to controlled thermal treatment in a muffle furnace under atmospheric conditions, with target temperatures selected on the basis of the thermal stability characteristics of each material. The residual ash content was determined gravimetrically after cooling the crucibles in a desiccator to constant weight.

2.1.2  Analysis of organic coating

The organic coating fraction was separated from the total material by solvent extraction using a 4:1 (v/v) dichloromethane/methanol mixture under reflux for four hours. The extracts were filtered through 0.45 µm PTFE membranes, concentrated under reduced pressure, and transferred to sample holders for subsequent spectroscopic characterisation by FTIR.

2.2  Sample preparation for elemental analysis (ICP-OES)

2.2.1  Sample preparation for optical emission spectrometry on total material

Approximately 0.25 g of each sample was digested in a closed-vessel microwave digestion system using a mixture of 6 mL concentrated nitric acid (HNO₃, 65%) and 2 mL hydrochloric acid (HCl, 37%). The digestion programme reached a maximum temperature of 200 °C and was held for 20 minutes. After cooling, the clear digests were quantitatively transferred and diluted to 50 mL with ultrapure water (≥ 18.2 MΩ·cm) prior to analysis.

2.2.2  Sample preparation for optical emission spectrometry on aqueous extract

A portion of each sample (approximately 5 g) was extracted with 100 mL of ultrapure water at 80 °C for two hours under continuous magnetic stirring. The extracts were cooled to room temperature, filtered through 0.22 µm cellulose acetate membrane filters, and acidified with 1 % (v/v) nitric acid to preserve dissolved species prior to ICP-OES analysis.

2.3  Sample preparation for the X-ray fluorescence analysis on the total material

Finely ground sub-samples were prepared by cryogenic milling to ensure complete homogenisation and a consistent particle size distribution below 50 µm. Approximately 4 g of the milled material was then pressed into 32 mm pellets using a hydraulic press operating at 15 tons for 60 seconds, with cellulose binder mixed in a 4:1 sample-to-binder ratio. The pressed pellets were analysed directly in the XRF instrument under vacuum conditions (< 10 mbar) using a rhodium anode X-ray tube operated at 50 kV and 40 mA.

3.  Results

3.1  Inorganic analysis

The inorganic constituents of the four submitted samples were characterised by ICP-OES and gravimetric analysis.

|  | WB Acrylic Emulsion Reference Standard #R5798; 020003954801 | WB Acrylic Emulsion #30084218501; 020003954803 | WB Acrylic Emulsion #30084218502; 020003954805 | WB Acrylic Emulsion #30084218503; 020003954807 |
| --- | --- | --- | --- | --- |
| Ash content (600 °C) [%] | 0.4 | 3.2 | 3.1 | 3.4 |

3.1.1  Composition of the total material

The following elements were detected by ICP-OES:

|  | WB Acrylic Emulsion Reference Standard #R5798; 020003954801 | WB Acrylic Emulsion #30084218501; 020003954803 | WB Acrylic Emulsion #30084218502; 020003954805 | WB Acrylic Emulsion #30084218503; 020003954807 |
| --- | --- | --- | --- | --- |
| Titanium (Ti) | 0.02 % | 1.78 % | 1.76 % | 1.81 % |
| Aluminium (Al) | 0.01 % | 0.18 % | 0.21 % | 0.15 % |
| Silicon (Si) | 0.04 % | 0.62 % | 0.59 % | 0.64 % |
| Calcium (Ca) | < 0.01 | 0.98 % | 1.02 % | 0.94 % |
| Magnesium (Mg) | < 0.01 | 0.07 % | 0.08 % | 0.06 % |
| Iron (Fe) | < 0.01 | 0.04 % | 0.05 % | 0.04 % |
| Zinc (Zn) | n.d. | 0.21 % | 0.19 % | 0.22 % |
| Sulphur (S) | < 0.01 | 0.42 % | 0.39 % | 0.44 % |

3.2  Binder characterisation and findings

The solvent extracts of the four submitted samples were characterised by FTIR. All four samples exhibited absorption profiles consistent with a waterborne acrylic emulsion. However, titanium content in the production batches (1.78 / 1.76 / 1.81 %) is below the historical baseline of 1.90–1.95 %, indicating reduced TiO₂ pigment loading. The reduction may produce visible colour and hiding-power variations vs. the reference. Recommended action: verify pigment metering calibration on the production line and review dispersion mill operating logs for the affected period.

Costs of analysis:  1,525.00 USD