ECO/TN   Karen O'Sullivan	ECO/AC

Dr. Samuel Whitaker

Tel.  +1 302 555-0148

Date  19-09-2025

Report-no:  US2025-0617

640000312418

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Titanium Dioxide Pigment / Reference (Current Production Grade); 020003961201

Titanium Dioxide Pigment / Candidate D — Ridgemont Industrial Pigments; 020003961203

Titanium Dioxide Pigment / Candidate E — Ironwood Mineral Solutions; 020003961205

Titanium Dioxide Pigment / Candidate F — Summit Chemical Inc.; 020003961207

Date of request:  05-09-2025

Receipt of order:  12-09-2025

1.  General introduction

On 19-09-2025, our laboratory received four samples of titanium dioxide (TiO₂) pigment for comparative supplier evaluation. The samples were submitted by Northbridge Coatings Inc. as part of a supplier qualification programme. The objective is to assess candidate suppliers against the incumbent production-grade reference for use in the 2K-PU clearcoat production line, with focus on metallic impurity profiles. The following investigations were performed:

- Determination of TiO₂ purity by gravimetric and ICP-OES analysis.

- Quantification of metallic impurities (Fe, Al, Si, V, Mn, Cr) by ICP-OES.

- Qualitative elemental confirmation by X-ray fluorescence (XRF).

- Particle size distribution and rutile/anatase ratio determination.

2.  Sample preparation

2.1  TiO₂ pigment digestion for ICP-OES

Approximately 0.20 g of each pigment sample was digested using a hot-block fusion approach with a mixture of concentrated sulphuric acid (4 mL) and ammonium sulphate (2 g) at 280 °C for 60 minutes. After cooling, the dissolved digests were diluted to 50 mL with ultrapure water for analysis.

2.2  Sample preparation for XRF

Pigment sub-samples were pressed into 32 mm pellets without binder using a hydraulic press at 20 tons. The pellets were analysed under vacuum conditions using a rhodium-anode X-ray tube.

2.3  Sample preparation for particle size and phase analysis

Aliquots of approximately 0.5 g were dispersed in deionised water with a non-ionic surfactant and sonicated for 5 minutes prior to laser diffraction measurement. Phase composition (rutile/anatase) was determined by X-ray diffraction on dry powder samples.

3.  Results

3.1  TiO₂ purity and impurity profile

The four titanium dioxide samples were characterised by ICP-OES (acid digest) and XRF qualitative analysis.

|  | Reference (Current); 020003961201 | Candidate D Ridgemont; 020003961203 | Candidate E Ironwood; 020003961205 | Candidate F Summit; 020003961207 |
| --- | --- | --- | --- | --- |
| Ash content (600 °C) [%] | 99.5 | 98.9 | 99.5 | 99.5 |

3.1.1  Composition and metallic impurity comparison

The following constituents were determined by ICP-OES:

|  | Reference (Current); 020003961201 | Candidate D Ridgemont; 020003961203 | Candidate E Ironwood; 020003961205 | Candidate F Summit; 020003961207 |
| --- | --- | --- | --- | --- |
| TiO₂ purity [%] | 99.51 | 98.91 | 99.51 | 99.51 |
| Iron (Fe) [%] | 0.08 | 0.42 | 0.08 | 0.08 |
| Aluminium (Al) [%] | 0.05 | 0.18 | 0.05 | 0.05 |
| Silicon (Si) [%] | 0.06 | 0.21 | 0.06 | 0.06 |
| Vanadium (V) [ppm] | 12 | 47 | 12 | 12 |
| Manganese (Mn) [ppm] | 8 | 31 | 8 | 8 |
| Chromium (Cr) [ppm] | 5 | 18 | 5 | 5 |
| Rutile content [%] | 94 | 89 | 94 | 94 |

3.2  Comparative supplier assessment

The four candidate samples were characterised in accordance with the standard supplier qualification protocol. The incumbent reference and acceptable candidates exhibit purity profiles within the established baseline (TiO₂ ≥ 99.5 %, iron ≤ 0.10 %). However, Candidate D — Ridgemont Industrial Pigments shows significantly elevated iron impurity at 0.42 %, more than 5-fold the incumbent baseline, accompanied by elevated aluminium, silicon, vanadium, manganese, and chromium. While the overall TiO₂ purity (98.9 %) remains acceptable for many applications, the elevated metallic impurity load is a concern: residual iron in TiO₂ feedstock has been observed historically to translate into measurable iron content in finished coatings, particularly in high-pigment-loading systems. Recommendation: Candidate D — Ridgemont Industrial Pigments should not be approved for the 2K-PU clearcoat production line without further finished-product impact assessment.

Costs of analysis:  2,240.00 USD