ECO/TN   Linda Brennan	ECO/AC

Dr. Samuel Whitaker

Tel.  +1 302 555-0148

Date  11-11-2025

Report-no:  US2025-0739

640000319214

Confidential – only for internal use!

Result of the analytical investigation of the samples:

Zn-Rich Epoxy Primer Reference Standard #R5984; 020003978401

Zn-Rich Epoxy Primer #30091347521; 020003978403

Zn-Rich Epoxy Primer #30091347522; 020003978405

Zn-Rich Epoxy Primer #30091347523; 020003978407

Date of request:  28-10-2025

Receipt of order:  04-11-2025

1.  General introduction

On 11-11-2025, our laboratory received four samples submitted by Apex Surface Solutions for routine batch release analysis. The samples comprise one reference standard and three production batches of zinc-rich epoxy primer intended for industrial and marine application. The objective of this analysis is to verify conformance with internal specifications and customer release criteria. The following investigations were performed:

- Determination of zinc content and metallic composition by ICP-OES.

- Determination of total ash content by gravimetric analysis.

- Qualitative elemental screening by X-ray fluorescence (XRF).

- Determination of chloride and sulphate by ion chromatography on aqueous extract.

- Characterisation of epoxy binder by FTIR.

2.  Sample preparation

2.1  Sample preparation for gravimetric and spectroscopic analysis

2.1.1  Examination of total material

Approximately 2 g of each sample was weighed into pre-ignited porcelain crucibles using a calibrated analytical balance with a readability of 0.1 mg. The samples were subjected to controlled thermal treatment in a muffle furnace under atmospheric conditions, with target temperatures selected on the basis of the thermal stability characteristics of each material. The residual ash content was determined gravimetrically after cooling the crucibles in a desiccator to constant weight.

2.1.2  Analysis of organic coating

The organic coating fraction was separated from the total material by solvent extraction using a 4:1 (v/v) dichloromethane/methanol mixture under reflux for four hours. The extracts were filtered through 0.45 µm PTFE membranes, concentrated under reduced pressure, and transferred to sample holders for subsequent spectroscopic characterisation by FTIR.

2.2  Sample preparation for elemental analysis (ICP-OES)

2.2.1  Sample preparation for optical emission spectrometry on total material

Approximately 0.25 g of each sample was digested in a closed-vessel microwave digestion system using a mixture of 6 mL concentrated nitric acid (HNO₃, 65%) and 2 mL hydrochloric acid (HCl, 37%). The digestion programme reached a maximum temperature of 200 °C and was held for 20 minutes. After cooling, the clear digests were quantitatively transferred and diluted to 50 mL with ultrapure water (≥ 18.2 MΩ·cm) prior to analysis.

2.2.2  Sample preparation for optical emission spectrometry on aqueous extract

A portion of each sample (approximately 5 g) was extracted with 100 mL of ultrapure water at 80 °C for two hours under continuous magnetic stirring. The extracts were cooled to room temperature, filtered through 0.22 µm cellulose acetate membrane filters, and acidified with 1 % (v/v) nitric acid to preserve dissolved species prior to ICP-OES analysis.

2.3  Sample preparation for the X-ray fluorescence analysis on the total material

Finely ground sub-samples were prepared by cryogenic milling to ensure complete homogenisation and a consistent particle size distribution below 50 µm. Approximately 4 g of the milled material was then pressed into 32 mm pellets using a hydraulic press operating at 15 tons for 60 seconds, with cellulose binder mixed in a 4:1 sample-to-binder ratio. The pressed pellets were analysed directly in the XRF instrument under vacuum conditions (< 10 mbar) using a rhodium anode X-ray tube operated at 50 kV and 40 mA.

3.  Results

3.1  Metallic composition and zinc content

The four samples were characterised by ICP-OES on acid digests for total metallic composition. All quantitative values are expressed as mass percentage (% w/w).

|  | Zn-Rich Epoxy Primer Reference Standard #R5984; 020003978401 | Zn-Rich Epoxy Primer #30091347521; 020003978403 | Zn-Rich Epoxy Primer #30091347522; 020003978405 | Zn-Rich Epoxy Primer #30091347523; 020003978407 |
| --- | --- | --- | --- | --- |
| Ash content (600 °C) [%] | 62.4 | 62.1 | 62.7 | 62.3 |

3.1.1  Elemental composition

The following elements were determined by ICP-OES:

|  | Zn-Rich Epoxy Primer Reference Standard #R5984; 020003978401 | Zn-Rich Epoxy Primer #30091347521; 020003978403 | Zn-Rich Epoxy Primer #30091347522; 020003978405 | Zn-Rich Epoxy Primer #30091347523; 020003978407 |
| --- | --- | --- | --- | --- |
| Zinc (Zn) | 82.4 % | 82.1 % | 82.6 % | 82.3 % |
| Iron (Fe) | 0.18 % | 0.21 % | 0.19 % | 0.22 % |
| Aluminium (Al) | 0.42 % | 0.41 % | 0.43 % | 0.40 % |
| Silicon (Si) | 0.61 % | 0.63 % | 0.60 % | 0.62 % |
| Calcium (Ca) | 0.08 % | 0.07 % | 0.08 % | 0.09 % |
| Magnesium (Mg) | 0.04 % | 0.04 % | 0.04 % | 0.05 % |
| Lead (Pb) | < 0.001 | < 0.001 | < 0.001 | < 0.001 |
| Cadmium (Cd) | < 0.001 | < 0.001 | < 0.001 | < 0.001 |

3.2  Ionic contamination — chloride and sulphate

Aqueous extracts of the four samples were analysed by ion chromatography for chloride and sulphate content, with supporting pH and conductivity measurements.

|  | Zn-Rich Epoxy Primer Reference Standard #R5984; 020003978401 | Zn-Rich Epoxy Primer #30091347521; 020003978403 | Zn-Rich Epoxy Primer #30091347522; 020003978405 | Zn-Rich Epoxy Primer #30091347523; 020003978407 |
| --- | --- | --- | --- | --- |
| Chloride (Cl⁻) | 0.04 mg/l | 0.11 mg/l | 0.09 mg/l | 0.10 mg/l |
| Sulphate (SO₄²⁻) | 0.12 mg/l | 0.14 mg/l | 0.13 mg/l | 0.13 mg/l |
| pH of aqueous extract | 8.4 | 8.5 | 8.4 | 8.5 |
| Conductivity [µS/cm] | 18 | 21 | 19 | 20 |

3.3  Binder characterisation and release determination

The solvent extracts of the four samples were characterised by FTIR. All four samples exhibited absorption profiles consistent with a bisphenol A epoxy resin binder system. Zinc content (82.1–82.6 %) exceeds the minimum specification of 80 %; iron content is well below limit; lead and cadmium are below the analytical detection limit, confirming RoHS compliance. However, chloride content in the production batches (0.11 / 0.09 / 0.10 mg/L) is at or above the 0.10 mg/L specification limit for offshore and marine application. Recommended action: review the production water supply chloride content and the rinse-water specification at the dispersion line. Batches at the spec boundary should be flagged for review before shipment to marine-environment applications.

Costs of analysis:  1,740.00 USD